450 Watts

MONOCRYSTALLINE SOLAR MODULE

Products features:

- Half Cut Bifacial Solar panel

- Strong aluminum alloy frame

- Standard tolerance (Guaranteed standard tolerance from -5~+5% ensures power output reliability)

- Excellent weak light performance

Excellent performance under low light environments (mornings, evenings, and cloudy days)

- Withstand high wind and snow loads

Entire module certified to withstand high wind loads (2400 Pascal) and snow loads (5400 Pascal)

| Model No. | SFM450W-108 |
| --- | --- |
| Maximum Power at STC (Pmax) | 450 W |
| Optimum Operating Voltage (Vmp) | 31V |
| Open - Circuit Voltage (Voc) | 37.2V |
| Optimum Operating Current (Imp) | 14.52A |
| Short - Circuit Current (Isc) | 15.97A |
| Operating Module Temperature | -40 °C to +85 °C |
| Maximum System Voltage | 1000V |
| Diodes | 3 by pass / 6 by pass |
| Power Tolerance | -5/+5% |

Mechanical Characteristics

| Solar Cell | Monocrystalline 166×83 mm |  |
| --- | --- | --- |
| No. of Cells | 108(2 ×54) |  |
| Dimensions | 1722*1134*30mm |  |
| Weight | 20.5Kgs |  |
| Front Glass | 3.2 mm (0.13 inches) tempered glass |  |
| Frame | Anodized aluminum alloy |  |
| Junction Box | IP68 rated |  |
| Output Cables | TUV |  |
|  | 4.0 mm2 (0.16inches2), symmetrical lengths (-) 22 mm 8.66 inches) and (+) 22mm (8.66inches) |  |
| Connectors | RADOX® SOLAR integrated twist locking connectors |  |

STC: irradiance 1000 W/m2, module temperature 25 °C, AM=1.5; Power measurement tolerance: ± 5%

Temperature Characteristics

| Nominal Operating Cell Temperature (NOCT) | 45±2 ℃ |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature Coefficient of Pmax | -0.47%/℃ |  |  |  |
| Temperature Coefficient of Voc | -0.34%/℃ |  |  |  |
| Temperature Coefficient of Isc | 0.045%/℃ |  |  |  |

uality and Safety:

Product warranty:

Singfo Solar modules will last for at least 25 years.

Free from defects in material and workmanship for 5 years.

All the panels passed IEC, TUV standards.

Power warranty:

Maintain more than 90% of minimum rated power for 10 years.

Maintain more than 80% of minimum rated power for 25 years.